

Method Statement

**Terraflex**

**Waterproofing Membrane System**

|  |  |
| --- | --- |
| **PREPARED FOR:** |  |
| **CONTRACT:** | Installation of allnex construction products;  **Terraflex Waterproofing Membrane System.**  Project: |
| **DATE:** | March 2023 |
| **SCOPE:** | 1. General Conditions of Contract. 2. General assessment and scope of work. 3. Pre-Start Execution. 4. Substrate requirements & surface preparation. 5. Pre-Installation Preparation. 6. Application Conditions. 7. Installation: allnex **Terraflex.** 8. Maintenance. 9. Cleaning. 10. Quality Assurance. 11. Protection Of Work. 12. Warranty. 13. Approved Installation Companies. 14. Documents to be consulted along with this specification. |
| **PREPARED BY:** | Colin Nolan  allnex construction products  Ph - +64 3 366 6802  Mob - +64 21 956 160  Email - [colin.nolan@allnex.com](mailto:colin.nolan@allnex.com)  [www.allnexconstruction.com](http://www.allnexconstruction.com) |
| **REFERENCES:** |  |

**1.0 GENERAL CONDITIONS OF CONTRACT**

1. All materials shall be installed using best trade practices and in accordance with the manufacturers recommendations or instructions. If any doubt exists please contact allnex Construction Products for advice.
2. Materials may only be installed by allnex approved applicators using staff skilled in the installation of all products covered by this specification. Applicators are to make available senior skilled staff to supervise the work while in progress.
3. The Applicator shall take reasonable steps to protect the general public, his work and adjacent surfaces during the time that his work is in progress.
4. Applicators are required to provide an acceptable Health and Safety programme which meets all the requirements of the current “Health & Safety in Employment” legislation. Applicators must also comply with any other relevant government legislation or local body laws, regulations or requirements.
5. The Applicator is to provide samples showing colour and finish for final approval by the client or his consultant prior to commencing work on site.
6. This specification is to be read in conjunction with relevant product information and conditions of contract which may be issued by the client.
7. The Applicator is to inspect all areas to be treated and must be satisfied that the surface is satisfactory to receive the proposed allnex system. If any doubt exists it is the responsibility of the Applicator to seek advice from allnex Construction products.
8. Any warrantee required will be supplied by the allnex approved applicator and backed up by our agreement with them.

*Refer: Section 12 below.*

1.9 allnex Q.A. procedure and documentation is to be accurately recorded and kept on site during the contract. allnex construction products reserves the right to inspect this documentation at any time. A copy of all relevant Q.A. information is to be returned to allnex within one month of completion of the work on site.

1.10 There shall be no substitute materials used unless written approval is provided by allnex Construction Products prior to the installation.

**2.0 GENERAL ASSESSMENT**

2.1 This specification has been prepared to detail the requirements and ensure client understanding as to the waterproofing system being proposed for the afore-named project by allnex Construction Products.

The correct installation will increase the durability, life expectancy and aesthetics of the facilities and will also provide site personnel with a safe working environment.

2.2 Applicators will be required to work closely with the main contractor and / or their designated co-ordinator / consultant to minimise disruption as a result of any work undertaken. Specific time requirements and logistics are to be negotiated directly between the Applicator and the main contractors authorised personnel.

2.3 Any change required during the course of the contract must be in writing.

2.4 The main contractor is to organise the removal of necessary equipment, plant etc prior to the commencement of the contract.

2.5 allnex Terraflex is a no odour option; however, all food or food packaging likely to be affected by the installation process (e.g. dust) should be removed from the area.

2.6 Provision for falls to drains, pre-filling etc. is to be discussed, priced and confirmed in writing, prior to the commencement of the contract. Repair any unsatisfactory falls, levels, etc. using STZ prefill system.

|  |  |
| --- | --- |
| **Falls** | |
| Roofs | 1:30 |
| Decks | 1:40 |
| Gutters | 1:100 minimum |

*Minimum Falls as above or as proscribed by local bodies or current legislation.*

*Confirm that the substrate, including falls, surface finish, fillets, sumps, countersinking terminations and projections, will permit Terraflex work of the required standard*.

*Falls:*

*The existing falls shall be checked in the following manner.*

1. *Around the perimeter of all walls, the levels shall be checked at maximum 500mm centres.*

*A continuous horizontal level shall be struck based on the highest point level found.*

1. *Where a level finish is called for the highest point level shall be found.*

*This point will determine the base point for the floor and the wall perimeter.*

*iii) Where falls are built into the substrate the difference between the lowest (waste) points and the highest (level determined under (i) and (ii) above) shall be checked against the levels proposed in the documents.*

*Should the Applicator find that the substrate requires remedial work before he can commence his application, then he shall request the Main Contractor to rectify the areas of defect.*

*Once the existing levels and proposed base levels are determined, the existing substrate shall be corrected (if required) using STZ Prefill. Refer: allnex STZ Prefill design document or consult allnex Construction Products for specific project advice..*

*Prefill shall be laid over all areas necessary to achieve the following results:*

*i) Around the perimeter of all walls and to all areas where a level floor finish is specified prefill shall be applied to provide a sub base level of +/- 3mm over a 3-metre grid.*

1. *To areas where a fall is specified prefill shall be applied to provide a sub base where a line laid between the high and low points shall be of constant gradient and very by no more than 3mm over a 3-metre length.*

2.7 All Terraflex installed and used as a finished flooring system is to comply with co-efficient of friction requirements to ensure compliance with current legislation.

2.8 If for any reason the Applicator is unable to carry out the installation of the allnex system in accordance with this specification, and relevant material data sheets, it is the responsibility of the Applicator to bring this to the attention of the client and / or allnex Construction Products in writing. This must be done prior to the commencement of the work.

2.9 The allnex Terraflex system is also suitable for upgrading and resurfacing existing sound membrane systems of the same type. *Consult allnex Construction Products for specific project advice.*

2.10 Applicators are required to clean up all debris etc from the work area once their work is completed.

2.11 Technical Data

Refer to *allnex Construction Website* for the latest technical literature.

***GUIDANCE NOTE***

***Use this clause when specifying by performance. Refer to the NZBC verification method D1/VM1 and acceptable solution D1/AS1. This clause may justify expansion, particularly where tiles are being laid in public areas.***

**2.12 Properties**

|  |  |  |
| --- | --- | --- |
| **Element** | **Values** | |
| Minimum Thickness: | 1mm DFT | |
| Minimum Application Temperature: Air | +10°C | |
| Maximum Application Relative Humidity: Air | 85% | |
| Terraflex System Steps: | *Refer Section: 2.13* | |
| Coving System: ~ Concrete  ~ Fibre-cement  ~ Plywood | Supaset  Supaset  Timber Fillet | |
| Cove upstand Detail: | As specified by Architect / Engineer | |
| Sealants: | SabreBond SMP60 | SabreSeal CR | |
| Pot-Life: ~ Aquakem | +250C ~ 75%RH | 2 hours |
| Surface Dry: ~ Aquakem | +250C ~ 50%RH | 2 hours |
| Hard Dry: ~ Aquakem | +250C ~ 50%RH | 24 hours minimum  *Allow 48 hours of cure prior to the application of the Terraflex membrane* |
| Body-coat: ~ Terraflex | +250C ~ 50%RH | > 4 hours between coats  *Dependent of weather condition* |
| Recoat : ~ Terraflex | +250C ~ 50%RH | Anytime within 24 hours.  *After 24 hours: Severe mechanical abrasion* |
| Foot Traffic:  *Finished System* | +250C ~ 50%RH | 24 hours |
| Full Use:  *Finished System* | +250C ~ 50%RH | >48 hours |
| Full Cure:  *Finished System* | +250C ~ 50%RH | 7 days |
| Recoat : | Anytime within 24 hours. | |
| *After 24 hours: Severe mechanical abrasion* | |
| Thinning: ~ Aquakem  ~ Terraflex | Do Not Thin  Do Not Thin | |
| Clean up: | All components clean up in water | |
| Dangerous Good Class: | Refer SDS sheets | |
| Packaging:  ~ Aquakem Resin  ~ Aquakem Hardener  ~ Terraflex  ~ Aquaglaze UV | 8 litre Unit | 20 litre Unit  4 litre | 10 litre  4 litre | 10 litre  15 litre plastic pail  10 litre plastic pail | |
| Shelf life: ~ Aquakem  ~ Terraflex | 6 months from date of manufacture  12 months from date of manufacture  *(After this period consult with allnex)* | |

**2.13 Terraflex System Steps**

|  |  |  |
| --- | --- | --- |
| **System Step** | **Component and Coverage** | **Component and Coverage**  **Heavy Duty Areas** |
| **Primer Coat**  **Coverage**  **Wet or Uncured Concrete**  **Coverage**  **1st Coat**  **2nd Coat** | Aquakem  5.0 m2 / Litre  Aquakem  3 m2/ litre  3 m2/ litre | Aquakem  5.0 m2 / Litre  Aquakem  3 m2/ litre  3 m2/ litre |
| **1st Body Coat**  **Coverage** | Terraflex  1m2  / litre | Terraflex  1m2  / litre |
| **Fibreglass Reinforcement** | 300gsm Chopped Strand Matt | 300gsm Chopped Strand Matt |
| **2nd Body Coat**  **Coverage** | Terraflex  3m2  / litre | Terraflex  3m2  / litre |
| **3rd Body Coat**  **Coverage** | Terraflex  6m2  / litre | Terraflex  1m2  / litre |
| **Fibreglass Reinforcement** | N/A | 300gsm Chopped Strand Matt |
| **4th Body Coat**  **Coverage** | N/A | Terraflex  3m2  / litre |
| **Topcoat**  **Coverage** | Terraflex  8 m2/ litre | Terraflex  8 m2/ litre |
| **Optional Clear Gloss Coat**  **Coverage** | Aquaglaze UV  10 m2/ litre | Aquaglaze UV  10 m2/ litre |

2.14 Trims and Edging

Refer project drawings for all trims, edging and termination detailing between resin floor finishes and other

## **3.0 PRE-START EXECUTION**

### 3.1 Storage

Accept all materials and accessories undamaged and dry. Store drums, pails and aggregates upright with other material on level surfaces in non-traffic, non-work areas that are enclosed, clean and dry and devoid of solar heat gain.

### 3.2 Handling

Avoid damage to drums and accessories.

### 3.3 Preparation

Record batches and stock numbers. Follow the allnex QA requirements for preparatory conditioning of materials working temperatures and conditions before, during and after application of the selected systems.

Protect the work from solar heat gain.

### 3.4 Do Not Start

Work shall not commence until the building is enclosed, all wet work is complete and good lighting is available.

For external applications protect the work area from adverse climatic conditions.

### 3.5 Inspect

Inspect the substrate to ensure it complies with the requirements of the selected finish system.

### 3.6 Protection

Protect adjoining work surfaces and finishes during the installation.

3.7 Site Safety

3.7.1 Ensure a site meeting has been held to acquaint other site workers with the requirement for closed access to the work area.

3.7.2 Ensure Health and Safety requirements are understood and agreed to prior to the commencement of the

contract.

3.7.3 Overalls are recommended when using this product.

### 3.8 Technique

Before beginning the installation confirm the proposed layout of material, location of control joints and other visual considerations of the finished work.

**4.0 SUBSTRATE REQUIREMENTS**

**4.1 New Concrete**

4.1.1 New concrete shall have a surface which has been mechanically trowelled to NZS3114:1987 U3 finish or better.

4.1.2 A minimum compressive strength of 25 MPA at 28 days cure..

4.1.3 A minimum cure time of 14 days.

4.1.4 Substrate Temperature ideally +10°C min / +40°C max, applications in lower temperatures will cause the material cure to become adversely affected.

4.1.5 Substrate Moisture Content: allnex Terraflex can be installed on substrates with a high moisture content. The substrate needs to be visibly dry and have a nominal pull-off strength of a min 1.5 N/mm2, with No ponding water.

***Wet & Uncured Concrete*** *(when less than 28 days cure).*

*Allow no further wetting.*

*The concrete design must be controlled for an early cure and low water content.*

*The Engineer must ensure that the concrete has a low water/cement ratio, is a high strength, rapid setting concrete containing water reducing agents and early cure agents.*

*It must be certified by the concrete placer that the above has occurred.*

*For the Warranty to apply; certification of the engineered concrete must occur and allnex Construction Products and its Applicator must see evidence of its formulation and correct installation.*

*Note*

*Two (2) Primer Coats of Aquakem at a spread rate of 3m2/litre/coat must be used in this instance*

*Refer: allnex Aquakem technical literature.*

4.1.6 All falls and levels to be accurately laid into the concrete. *Refer: 2.6 above.*

4.1.7 A suitable vapour resistant membrane beneath the concrete slab is required.

4.1.8 A surface free of cement laitance or other contaminants and any roughly screeded or floated areas. No traces of cure membranes

4.1.9 Deep depressions, impact damage, hollows etc to be repaired or filled as appropriate using Surecote 500 Prefill or allnex Supaset

4.1.10 Repair any unsatisfactory falls, levels, etc using Surecote 500 Prefill or Polymer Screed - allnex Screed 20**+** as appropriate to suit the proposed floor finish.

**4.1.11 New Concrete Surface Preparation**

|  |  |
| --- | --- |
| **allnex recommend mechanical abrasion techniques as the surface preparation method.** | |
| Preferred Option | Captive Shot blasting |
| Secondary Option | Diamond Grinding |
| Minimum Requirement | CSP 3 |
| *Refer: allnex Surface Preparation Technical Literature* | |

**4.2 Existing Concrete**

4.2.1 Ensure existing concrete is sound and stable with a minimum compressive strength of 25 MPA.

4.2.2 Substrate Moisture Content: allnex Terraflex can be installed on substrates with a high moisture content. The substrate needs to be visibly dry and have a nominal pull-off strength of a min 1.5 N/mm2, with No ponding water.

4.2.3 Remove all contaminants including cement laitance, dirt, grease, oil, fats, existing coatings, unsound substrate etc by steam cleaning, captive shot blasting, grinding, scabbling, hammering etc as appropriate.

4.2.4 All falls and levels to be accurately laid into the concrete. *Refer: 2.6 above*

4.2.5 A suitable vapour resistant membrane beneath the concrete slab is required.

4.2.6 A surface free of cement laitance or other contaminants and any roughly screeded or floated areas. No traces of cure membranes.

4.2.7 Cracks in the concrete are to be bandaged using allnex 300gsm fibreglass slip tape bandage or treated as a control joint as appropriate.

4.2.8 Deep depressions, impact damage, hollows etc to be repaired or filled as appropriate using Surecote 500 Prefill or allnex Supaset.

4.2.9 Repair any unsatisfactory falls, levels, etc using Surecote 500 Prefill or Polymer Screed – Screed 20**+** as appropriate to suit the proposed floor finish.

**4.2.10 Existing Concrete Surface Preparation**

|  |  |
| --- | --- |
| **allnex recommend mechanical abrasion techniques as the surface preparation method.** | |
| Preferred Option | Captive Shot blasting |
| Secondary Option | Diamond Grinding |
| Minimum Requirement | CSP 3 |
| *Refer: allnex Surface Preparation Technical Literature* | |

**4.3 Plywood | Fibre-cement**

*Note*

*Wherever possible prime the Plywood and Fibre-cement with Aquakem prior to sheet installation.*

*Pay particular attention to the edges of the sheets.*

**4.3.1** **Plywood Sheet:**

|  |  |
| --- | --- |
| **Element** | **Value** |
| Framing: | All framing must comply with current legislation.  Framing must take into consideration all loading parameters. |
| Plywood: | Must Comply with AS/NZS2269. |
| Plywood Type: | H3.2 treated CCA (water-based treatment) with a square edge. |
| Plywood Thickness: | Floors: 17mm – Minimum.  Walls : 12mm – Minimum. |
| Plywood Installation: | Loose butted. |
| Plywood Fastening Type: | Corrosion resistant screws - preferably 50mm stainless screws. |
| Fastening Spacings: | Perimeter: 150mm.  Centres: 200mm. |
| Countersink Fastening: | All fastenings must be countersunk 0.5mm. |
| Filling of Countersunk Fastenings: | Flush fill all screw heads and sheet joints using allnex Fairing Cream. |
| Plywood Sheet Joints: | All joints must be left with a uniform finish. |

**4.3.2 Fibre Cement Sheet**

|  |  |
| --- | --- |
| **Element** | **Value** |
| Framing: | All framing must comply with current legislation  Framing must take into consideration all loading parameters. |
| Fibre Cement: | Must Comply with AS/NZS2269 |
| Fibre Cement Type: | With rebated edges that can be stopped to flush the joints. |
| Fibre Cement Thickness: | Floors: 18mm - Minimum  Walls : 9mm – Minimum |
| Fibre Cement Fastening Type: | 316 Stainless Screws - 50mm x 10g |
| Fastening Spacings: | Perimeter: As per manufacturer’s instructions  Centres: As per manufacturer’s instructions. |
| Countersink Fastening: | All fastenings must be countersunk as per Manufacturer’s instructions. |
| Filling of Countersunk Fastenings: | Flush fill all screw heads and sheet joints using allnex Fairing Cream. |
| Fibre Cement Sheet Joints: | All joints must be left with a uniform finish. |

Note

In all cases:- Refer to the Manufacturer’s installation instructions.

**5.0 PRE - INSTALLATION PREPARATION**

5.1 Round all edges at downturns.

5.2 Install fillets at floor to wall junctions.

5.3 Ensure Drains / vents & overflows are rebated and installed correctly.

5.4 Ensure Flashings and the correct installation of movement/control joints has been achieved.

**6.0 APPLICATION CONDITIONS:**

6.1 Products such as Terraflex require *good drying conditions*to allow water to evaporate from the coating.

6.2 *Do not* apply in temperatures less than 10°C or when wet weather is likely.

6.3 Good *air movement*is the best method of drying water-based products.

6.4 Working in hot, dry windy conditions will be difficult as the material will setup too rapidly.

*Study weather forecasts to ensure that the material will be fully through dry prior to any rain.*

## **7.0 INSTALLATION OF ALLNEX TERRAFLEX WATERPROOFING MEMBRANE FINISH**

*Note Well*

*It is important that more thinner coats are applied, rather than fewer thicker coats.*

*Excessively thick coats retard drying and may lead to blisters*

7.1 Ensure the substrate is properly prepared and is suitable to receive the allnex Terraflex finish.

7.2 Neatly mask out and protect all areas not covered by the proposed work.

**7.3 Primer Application**

|  |  |
| --- | --- |
| **Primer Type** | |
| **Metal** | Anti-corrosion metal primer  Follow with Aquakem |
| **Concrete | Plywood | Fibre-cement** | Aquakem |

|  |  |
| --- | --- |
| **Aquakem Mixing Ratio** | |
| **Maximum coverage 5m²/litre/coat.** | |
| **Aquakem Part A** | 1 part |
| **Aquakem Part B** | 1 part |

|  |
| --- |
| **New Wet Concrete Installation** |
| **Maximum coverage 3m²/litre/coat.**  **2 x Coats Required**  **Refer: Aquakem Technical Literature** |

7.3.1 Aquakem Part A | Part B are to be thoroughly mixed in the correct proportions. Refer: *Aquakem Technical Literature*

7.3.2 Mix for a minimum of 3 minutes at 200-300rpm. *Refer: Aquakem Technical Literature*

7.3.3 Apply a minimum one coat of Aquakem by brush and roller ensuring it is worked well into the prepared substrate, including joints of a Plywood or Fibre-cement substrate.

7.3.4 Coverage rate and number of coats of Primer will vary depending on the porosity of the substrate.

7.3.5 Allow primer to fully cure.

7.3.6 Porous areas may require further coats until porosity is eliminated.

*Note*

*Allow Aquakem to cure for a minimum of 48 hours*

**7.4 Plywood and Fibre-cement Sheet Joints and Upstand Reinforcement**

7.4.1 All joints should be Fibreglass taped prior to the full membrane application.

7.4.2 Install allnex Joint Safe Tape at all floor/wall junctions.

7.4.3 Sheet Joints will require a 100mm wide strip of 300gsm chopped strand fibreglass matt or polyester cloth tape.

*Note*

*The polyester cloth tape will dry more quickly than the chopped strand mat.*

7.4.4 Wider strips will be needed to form coves.

7.4.5 In all cases, apply a heavy coat of Terraflex body coat and lay in the CSM strip and apply a further body coat. Immediately use a metal laminating-roller (refer: to allnex range) to bring the body coat up through the CSM.

7.4.6 Use a garden sprayer to apply a *fine water mist.*

*This ensures that the Terraflex is fluid and wets the glass readily.*

7.4.7 Allow to fully dry (*test),* prior to the full membrane installation.

**7.5 Fibreglass Reinforcement Preparation**

|  |  |
| --- | --- |
| **Element** | **Value** |
| Fibreglass Salvage edge: | The salvage edge of the fibreglass matt must be “teased’ prior to installation. |

7.5.1 The “teasing” of the salvage edge assists with the overlap application.

**7.6 Terraflex Body Coats & Reinforcement**

7.6.1 Once the sheet joint reinforcing has cured, apply evenly by way of roller / brush the first body-coat of Terraflex to the area to be laid up.

A wet edge must be maintained across the work face to allow the next section of Terraflex to be worked in without showing a ridge.

*Note*

*Use a long nap roller to ensure an even coverage and that enough material is used to ensure a complete “wet out” of the fibreglass matt.*

7.6.2 Install the pre – prepared 300gsm chopped strand matt into the wet resin body-coat.

*Note*

*The fibreglass is to have a minimum 75mm minimum overlap*

7.6.3 The fibreglass matt is to be worked with a “Parsley Cutter*” (laminating roller)* to bring the resin through the matt thus ensuring a complete “wetting out” of the inside of the fibreglass chopped strand matt.

7.6.4 Use a garden sprayer to apply a *fine water mist.*

*This ensures that the Terraflex is fluid and wets the glass readily*

*Critical Step*

*If there is not enough Terraflex on the substrate surface prior to the installation of the 300gsm chopped strand matt it will be difficult to obtain a full “wet out” of the matt.*

*Applying more Terraflex to the surface and trying to work it back into the matt will cause a dry laminate finish and is unacceptable.*

7.6.5 The sufficient quantity is indicated by surplus spots being forced up by the action of the roller.

7.6.6 Apply the second coat of Terraflex wet on wet and roll evenly.

Allow these coats to dry (test thoroughly dry)

7.6.7 Apply third coat of Terraflex.

*Note*

*This coat must be applied at “right angles” to the previous Body coat and take care to ensure that the Terraflex is worked into all areas with particular attention being paid to all internals and externals*

Note

If a higher degree of non-slip profile is required apply the third Body coat applied by way of a “goop loop” roller.

**7.7 Upstands and walls**

7.7.1 Once the main area has cured and is able to be trafficked, install Terraflex and 300 gsm fibreglass reinforcement to all upstands / walls.

*Note*

*Ensure the Fibreglass reinforcement overlaps onto the deck by a 75mm minimum.*

7.7.2 Allow all areas of reinforced Body coat to cure and check for shrinkage cracks and pinholes.

*Note*

*If a smoother finish is required on upstand areas it is recommended that the use of surfacing tissue be incorporated into the system.*

**7.8 HEAVY DUTY AREAS:**

7.8.1 Include a second layer of mesh in the 3rd body coat of Terraflex and add a 4th coat of Terraflex to the system.

This markedly improves wear and impact resistance.

7.8.2 Edge and step details may be further reinforced in this way.

**7.9 Topcoats**

7.9.1 Allow all areas to fully cure and apply the final colour coat at the correct coverage rates. *Refer: section 2.13*

***Optional***

7.9.2 An optional Aquaglaze UV clear glaze coat may be applied at this time. This will aid cleaning and longevity of the system by adding a gloss which will assist in reducing scuffing. *Refer: section 2.13*

*Note*

*These coats must be applied at “right angles’ to the previous coats.*

**Observe minimum / maximum re-coat recommendations**

**8.0** **MAINTENANCE**

● Inspect yearly.

● Membrane peaking is indicating deck movement - Inspect.

● Re-apply Terraflex as appropriate.

● Low wear decks should be recoated every 5 years with Terraflex.

● Do not allow wear to damage fibres of the CSM material

● Ease of repair is a major advantage with the allnex Terraflex membrane.

● Damaged areas are cut out and repaired using new materials quickly and with little disruption.

**9.0 CLEANING**

*Refer: Cleaning and Maintenance Technical Literature on the allnex Construction Website.*

**10.0 QUALITY ASSURANCE**

A log shall be kept by the approved applicator and made available to allnex at their request.

Information to be recorded daily is but not limited to:-

* Material Batch Numbers
* Sequence of Mixing ratios and quantities and formula
* Substrate Moisture Content
* Substrate Temperature
* Ambient Temperature
* Ambient Relative Humidity

**11.0 COMPLETION & PROTECTION OF WORK**

The approved Applicator shall take reasonable steps to protect his work and the work of others trades during the time that his work is in progress.

The General Contractor during the same time shall keep the areas free and clear of traffic. Thereafter, until the building is completed.

It shall be the responsibility of the General Contractors to protect the allnex membrane from damage, paint droppings, or other contamination that may prove difficult to remove or detrimental to the finished membranes characteristics and performance.

The approved Applicator shall:

* Check membrane has sealed all surfaces.
* All cove details are full and complete with no gaps that may allow water ingress.
* Check non-slip surface texture is as specified and even.
* Check all water falls to drains, with no ponding as specified.
* Ensure floor / topcoat is fully cured overnight prior to other trades or service.
* Check all areas to ensure that all flashings are installed correctly.

**12.0** **WARRANTY**

allnex will assure that all products incorporated into this specification have been manufactured to allnex quality specifications and GMP procedures.

allnex will also assure that when correctly applied the system will meet the critical requirements of the allnex design specification.

However, given that allnex has no control over the substrate, the application environment and the application process all warranties are supplied by the approved Applicator and backed by our agreement with them.

The approved Applicator shall provide a warranty for a period of:

**Fifteen (15) Years**

The warranty period commences from the date of practical completion.

Damaged areas must be repaired immediately to ensure continuity of the Warranty

*Note\**

*The user should note that “wrinkling or seaming” is due to substrate movement*

*The warranty is supported by allnex Construction Products.*

**13.0 ALLNEX APPROVED REGIONAL INSTALLATION COMPANIES**

allnex will provide individual advice for specific projects and should be consulted.

It is the nature on the trade that contractor skill levels, capability and experience vary.

**14.0 DOCUMENTS TO BE CONSULTED**

● allnex Approved Applicator List  ● allnex Exterior Installation

● allnex Product Technical Data Sheets ● allnex Colour Formulas

● allnex Waterproofing Details● allnex Cleaning Recommendations

● allnex Surface Preparation Document● allnex Technical Bulletins

*GUIDANCE NOTE*

*Include cross references to other sections where these contain related work.*

**Date: March 2023**

**Replaces February 2023**



**allnex Construction Products, a Division of allnex New Zealand Ltd**

**Auckland** – 14 Industry Road, Penrose. phone: 09-583-6544.

**Hamilton** - 18 Somerset Street, Frankton. phone: 07-847-8658.

**Wellington –** Unit 9A, 4 Glover Street, Ngauranga Gorge. phone: 04-240-0305.

**Christchurch** – 112 Carlyle Street, Sydenham. phone: 03-366-6802.

**Customer Service: 0508-882-288** [**cs.constructionnz@allnex.com**](mailto:cs.constructionnz@allnex.com)

[**www.allnexconstruction.com**](http://www.allnexconstruction.com)

**DISCLAIMER:** This information appearing in this Document (**Details**) concerning the product which is the subject of the Document (**Product**) is either based on present technical knowledge and tests done by allnex or tests done by, and data supplied from third parties including you, the customer. Since the actual use by you and by others of the Product is beyond the control of allnex, no warranty or representation, express or implied is made by allnex regarding the suitability for such use, nor does allnex accept any liability arising out of the use by you of other products or materials, whether third party or not, that may be referred to in this Document. allnex recommends that you carry out your own tests as to the suitability of the Product for your purpose, regarding which you accept full responsibility. In addition, if any of the Details appearing in the Document are based upon tests done by, and/or data supplied by any third party, allnex provides no warranties or representations in connection with those Details and you, the customer waives any right you may have against allnex in connection with the accuracy, completeness or otherwise of the Details. The information in this Document is not to be construed as absolutely complete or accurate since additional information may be necessary or desirable when particular or exceptional conditions or circumstances exist or because of applicable laws or government regulations affecting use of the Product. allnex does not provide any warranty or representation to you that the Product does not infringe the intellectual property rights of any third party. All orders accepted shall be subject to the standard conditions of sale of allnex which are on the back of our invoice. In accepting the Product, you, the customer acknowledge and agree: **a.)** The Product is or may be of a hazardous nature and that you, the customer, are responsible for the disposal of the container housing the Product in accordance with the requirements and regulations of the relevant supervising government**. b.)** The Product has a limited shelf life and must be stored strictly in accordance with the guidelines and specifications related to it. **c.)** Where the Details relate to Product tested by allnex, those Details are indicative only, regarding which there may be batch to batch variation. **d.)** allnex gives no warranty or representation as to the applicability for the particular use by you, the customer, of the Product and you the customer shall be responsible for ensuring that the Product is fit for your intended use. **e.)** allnex’s liability for breach of any term, condition, guarantee or warranty (express or implied and concerning the information in this Document or the Product more generally) including any liability for direct or indirect consequential loss (including indirect loss of profits), is limited to the maximum extent permitted by law and, at allnex’s election, to either replacing or repairing the goods or paying the cost of replacing or repairing the goods, or in the case of services, supplying the services again.

**©2017 allnex Group. All Rights Reserved.**